Problem 2 (3 points)

A body-centered cubic lattice has a lattice constant of 4.83 Å. A plane cutting the lattice has intercepts of 14.49 Å, 9.66 Å, and 28.98 Å along the three Cartesian coordinates (x, y, and z). What are the Miller indices of the plane?

Solution:

x,y,z=14.49, 9.66, 28.98

h, k, l=114.49,19.66,128.98*4.83→13,12, 16 →(2, 3, 1)

PROBLEM No 3: (2+1+2 =5 points)

If the lattice constant of silicon is 5.43 Å, calculate

(a) the distance from the center of one silicon atom to the center of its nearest neighbor,

(b) the number density of silicon atoms (#/cm3 ), and

(c) the mass density (g/cm3 ) of silicon (check if it matches with the density of Si).

Solution:

(a)

d=143a=143*5.43≅ 2.35125897Å

(b)

85.43*10-83=4.9967831022687*1022atomscm3

(c)

# of atoms=Avogardo NumberMolecular Weight→6.0221*102328.0855≅2.1442*1022

4.9967831022687*10222.1442*1022≅2.33gcm3

Problem No. 4 (1+1+1+1 = 4 points)

The crystal structure of sodium chloride (NaCl) is a simple cubic with the Na and Cl atoms alternating positions. Each Na atom is then surrounded by six Cl atoms and likewise each Cl atom is surrounded by six Na atoms.

(a) Sketch the atoms in a (100) plane.

(b) Assume the atoms are hard spheres with nearest neighbors touching. The effective radius of Na is 1.0 Å and the effective radius of Cl is 1.8 Å. Determine the lattice constant.

(c) Calculate the volume density of Na and Cl atoms.

(d) Calculate the mass density of NaCl.

[Note: Na +: atomic weight 22.99g/mol, radius 1Ǻ , and Cl -: atomic weight 35.45g/mol, radius 1.8Ǻ]

Solution:

- a=rCl+rNa=1.8Å+1Å=2.8Å

a=2.8*10-8cm

Na Atom Density=0.5 atoms2.8*10-83≅2.2777*1022

Cl Atom Density=0.5 atoms2.8*10-83≅2.2777*1022

Na # of atoms=Avogardo NumberMolecular Weight→6.0221*102322.99≅2.619*1022

2.2777*10222.619*1022≅0.869683gcm3

Cl # of atoms=Avogardo NumberMolecular Weight→6.0221*102335.45≅1.69876*1022

2.2777*10221.69876*1022≅1.34gcm3

1.34gcm3+0.869683gcm3=2.21gcm3

Question No. 5 (5 points):

Write production process of Silicon wafers starting from sand [silicon dioxide (SiO2)]

Very pure sand is generally wanted for silicon production, so that there are less steps to do later.

The sand is heated to about 1600° C, just above it’s melting point, and the impurities can be removed.

After the sand has been purified and converted into pure Si, it is melted again.

A “seed crystal” is placed in the molten sand and is pulled out slowly while being rotated.

Question No. 6 (3 points):

What is the significance of epitaxial growth processes? Which epitaxial growth process is mostly used by the industry and why by comparing the two mostly used processes?